Study of the charge density wave of NbSe2 by STM/STS
Christian Lupien
Behnaz Behmand
Université de Sherbrooke
Thomas T.M. Palstra
University of Groningen (Netherlands)

---
Outline
The problem of identifying a CDW
Overview of NEW STM installation
Results so far...
Conclusion

---
The CDW problem

---
The CDW problem
CDW = Charge density wave
  - Real space charge modulation
The problem is with measurements on the high-Tc superconductors (cuprates)
  - STM/STS show many structures
  - Complicated system (phase diagram)
  - Are some of them CDW? Or are they pair-density waves, or ...

---
STM/STS on NaCCOC

---
Spectroscopic imaging within pseudogap (Conductance Maps)
Spectroscopic imaging within pseudogap
(Conductance Maps)
5 nm
x ~ 0.10
T. Hanaguri et al., Nature 430, 1001 (2004)
Topograph
T ~ 100 mK
Vsample = 200 mV
It = 50 pA
1 Å
dI/dV|+24mV
T ~ 100 mK
Vsample = 200 mV
It = 100 pA
0.47 nS

---
Theory of identification of CDW
The density of states (DOS) should be anti-symmetric vs energy for a pure CDW (and not for some other theories)
  - i.e. More holes = Less electrons
STM/STS conductance is proportional to the DOS
Therefore the STS conductance map should be able to identify the presence of a pure CDW.

---
Model
DOS
Average
Holes
Electrons
0
Fermi Energy
Energy

---
In practice
Fourier Transform the local DOS
The k=0 signal gives the averaged DOS
The k vector of the CDW should give :
Phase
Jump of 180 degree
Energy

---
NbSe2
Since cuprates are complicated systems
  - Want to check ideas/analysis on something simpler
Choose NbSe2
  - A well known CDW material (TCDW ~ 33K)
  - Also a superconductor (TC ~ 7K) (unnecessary here)
  - Surface prepares easily
  - Not fully understand (but better than cuprates) and very well characterized

---
Tour of the lab 2006
Big hole (10 feet), filled with concrete

---
Tour of the lab
Pumping lines
vibration
isolation
1 ton lead
Air piston
20 ton concrete
on rubber
15-17 T magnet

---
He3 cryostat + Microscope
Sample preperation:
cleaving

---
Microscope
Un microscope en morceux...

---
Microscope
Coeur du microscope
Piezo XYZ et
porte-pointe
Corps du marcheur
Pointe de Tungstène
8mm

---
Microscope
Condensateur

---
Tip-Sample Tunneling Current
Apply a voltage V
lowers EF of sample by eV
with respect to EF of tip

---
Tip-Sample Tunneling Current
color red {dI prop "LDOS"(E)dV}
color red { drarrow dI over dV prop "LDOS" (E)}

---
NbSe2 Topograph
0.5 Å
-0.5 Å
Single defect
→good tip!
20 x 20 nm -100 mV/100 pA
[Speaker Notes: 81125A09]

---
Other topograph
0.5 Å
-0.3 Å
CDW ~ 3 ao
10 x 10 nm -100 mV/100 pA
[Speaker Notes: 81120A04]

---
Another topograph
0.6 Å
-0.5 Å
10 x 10 nm -100 mV/100 pA
[Speaker Notes: 81203A02]

---
Average spectra @ 450 mK
Charge density wave
Superconducting Gap
Bias Voltage (mv)
Conductance (nS)

---
Conductance Map

---
Conductance Map

---
Fourier transform of map (+100mV)
Atoms
CDW
~1/3

---
Filtered Conductance map
We keep only the CDW vectors (remove atomic vectors, harmonics)

---
Filtered Conductance map
We keep only the CDW vectors (remove atomic vectors, harmonics)

---
Cross-correlation (ref = 20 mV)
It crosses 0
BUT at 40mV
+1 means fully in-phase
-1 means fully out of phase
0 is either in-between phase or noise (no correlation)

---
Problem: set-point effect
We scan with feedback: keep current constant.
This changes the proportionality constant between conductance (g) and DOS
It forces a sign change on all g(k,E) for k≠0 on the E side of the setpoint
Solutions?
  - Remove the constant at each pixel by analyzing instead Z =g(+E)/g(-E) and then FFT
  - If signal disappears and average curve is symmetric than signal was symmetric vs energy

---
Fourier transform of map (+100mV)
Atoms
CDW
~1/3

---
Fourier transform of Z map (+100 mV)
Very usefull Trick, but does not help much the comparison with theory?

---
Conclusions
Working STM – Open for business
Extracting energy symmetry at particular wavevector is hard even for the simpler NbSe2
  - Effect of setpoint
  - Effect of atomic displacement on the spectra...